J30	LIQUID APPLIED TANKING / DAMP PROOFING

To be read with Preliminaries / General conditions.

TYPES  OF  TANKING / DAMP  PROOFING

J30/130	COLD APPLIED DAMP PROOFING

-	Substrate : …………………

- Primer : RIW Flexiseal Pro Primer ; two-pack

-   Application : Number of coats : 1 No. minimum  – see Clause 207 below

Coverage per coat ( minimum ) : 4m² / litre.

-	Coating : Polymer modified epoxy

-   Manufacturer : RIW Limited, Arc House, Terrace Road South, Binfield, RG42 4PZ.

Tel : 01344  397777   Fax : 01344  862010

E-mail : technical@riw.co.uk   Web : www.riw.co.uk

Product reference : RIW Flexiseal Pro ; two-pack

-	Application : Number of coats : 1 No. Horizontally - 2 No. Vertically

Coverage per coat (minimum) : 1 m² / kg - Horizontal

2 m2 / kg - Vertical

-	Reinforcement : Not required.

or

-	Reinforcement : Embed Flexiseal Pro Scrim between two layers of Flexiseal Pro, laid wet on wet, where required / specified.

-	Blinding : Not required.

EXECUTION

J30/205	SUITABILITY OF SUBSTRATE

-	Substrates generally :

-	Smooth, even textured, clean, dry and frost free.

-	Within tolerances for level and surface regularity.

-	Vertical and horizontal surfaces : Correctly prepared and free from irregularities.

-	Moisture content and stability of substrate : Must not impair integrity of finished tanking / damp proofing.

-	Preliminary work : Complete including :

-	Chases.

-	External angles.

-	Formation of upstands and kerbs.

-	Movement joints.

-	Penetrations / Outlets.

J30/207	PRIMERS

- Application : Uniform, continuous coverage.

- Apply 2nd coat, when applied onto very porous surfaces.

J30/210	COATING APPLICATION

- Adjacent surfaces exposed to view in finished work : Protect.

-	Coatings :

-	Apply in dry atmospheric conditions when primer is tacky. Allow to dry when used on bituminous surfaces.

-	Uniform, continuous coverage. Do not allow to pool in hollows.

-	Firmly adhered to substrate and free from imperfections.

-	Prevent damage to finished coatings.

-	Penetrations : Impervious.

- Final covering : Apply as soon as possible after coating has hardened.

J30/220	COLD APPLIED COATINGS

-	Thinning : Not permitted unless recommended by manufacturer.

-	Successive coats :

-	Allow to dry before applying next.

-	Apply at right angles to previous.

J30/235	MODIFIED COATINGS

-	Air and surface temperatures : Do not apply if below minimum recommended by coating manufacturer.

-	Curing: Keep dry until fully cured.

J30/260	JUNCTIONS WITH DPC’s

-	DPC’s: Clean, all edges fully exposed.

-	Application : Fully coat dpc, and overlap adjacent surfaces by ( minimum ) 75mm.