J30	LIQUID APPLIED TANKING / DAMP PROOFING

To be read with Preliminaries / General conditions.

TYPES  OF  TANKING / DAMP  PROOFING

J30/110 	COLD APPLIED TANKING

-	Substrate : …………………

- Primer : RIW Flexiseal Pro Primer ; two-pack

-   Application : Number of coats : 1 No. minimum – see Clause 207 below

Coverage per coat ( minimum ) : 4m² / litre.

-	Coating : Polymer modified epoxy

-   Manufacturer : RIW Limited, Arc House, Terrace Road South, Binfield, RG42 4PZ.

Tel : 01344  397777   Fax : 01344  862010

E-mail : technical@riw.co.uk   Web : www.riw.co.uk

Product reference : RIW Flexiseal Pro ; two-pack

-	Application : Number of coats : 1 No. Horizontally - 2 No. Vertically

Coverage per coat (minimum) : 1m² / kg - Horizontal

2m2 / kg - Vertically

-	Reinforcement : Not required.

or

-	Reinforcement : Embed Flexiseal Pro Scrim between two layers of Flexiseal Pro, laid wet on wet, where required / specified.

EXECUTION

J30/205	SUITABILITY OF SUBSTRATE

-	Substrates generally :

-	Smooth, even textured, clean, dry and frost free.

-	Within tolerances for level and surface regularity.

-	Vertical and horizontal surfaces : Correctly prepared and free from irregularities.

-	Moisture content and stability of substrate : Must not impair integrity of finished tanking / damp proofing.

-	Preliminary work : Complete including :

-	Chases.

-	External angles.

-	Formation of upstands and kerbs.

-	Movement joints.

-	Penetrations / Outlets.

J30/207	PRIMERS

- Application : Uniform, continuous coverage.

- Apply 2nd coat, when applied onto very porous surfaces.

J30/210	COATING APPLICATION

- Adjacent surfaces exposed to view in finished work : Protect.

-	Coatings :

-	Apply in dry atmospheric conditions when primer is tacky. Allow to dry when used on bituminous surfaces.

-	Uniform, continuous coverage. Do not allow to pool in hollows.

-	Firmly adhered to substrate and free from imperfections.

-	Prevent damage to finished coatings.

-	Penetrations : Impervious.

- Final covering : Apply as soon as possible after coating has hardened.

J30/220	COLD APPLIED COATINGS

-	Thinning : Not permitted unless recommended by manufacturer.

-	Successive coats :

-	Allow to dry before applying next.

-	Apply at right angles to previous.

J30/235	MODIFIED COATINGS

-	Air and surface temperatures : Do not apply if below minimum recommended by coating manufacturer.

-	Curing : Keep dry until fully cured.

COMPLETION

J30/330	PROTECTION OF COATINGS

-	Coated surface : Clean and free from contaminants.

-	Board manufacturer :

RIW Limited, Arc House, Terrace Road South, Binfield, RG42 4PZ.

Tel : 01344  397777   Fax : 01344  862010

E-mail : technical@riw.co.uk   Web : www.riw.co.uk

-	Product reference : RIW Double Drain

-	Thickness : 8mm.

-	Placement : Immediately prior to covering. Provide support as necessary.

-	Edges :  70mm minimum overlap.

-	Perimeter treatment : Seal with geotextile fabric to  prevent silt entering the core.

-	Contact with coating : Secure and continuous.

or

-	Product reference : RIW Protection Board.

-	Thickness : 3mm.

-	Placement : Immediately prior to covering. Provide support as necessary.

-	Edges : Butt jointed and taped.

-	Perimeter treatment : Not required.

-	Contact with coating : Secure and continuous.

J30/340	BACKFILLING TO EXTERNAL COATINGS

-	Timing : Carry out as soon as possible after tanking and protection are complete.