J30	LIQUID APPLIED TANKING / DAMP PROOFING

To be read with Preliminaries / General conditions.

TYPES OF TANKING / DAMP PROOFING

J30/130 	COLD APPLIED DAMP PROOFING

-	Substrate : …………………

-	Primer : Not required.

-	Coating : Modified epoxide coating.

- Manufacturer : RIW Limited, Arc House, Terrace Road South, Binfield, RG42 4PZ.

Tel : 01344  397777   Fax : 01344  862010

E-mail : technical@riw.co.uk   Web : www.riw.co.uk

-	Product reference : RIW Toughseal.

-	Application : Number of coats : Two ( 2 )

Coverage per coat (minimum) : 4m² / litre.

-	Reinforcement : RIW Flexiseal, in accordance with manufacturer’s recommendations.

or  where a tiled finish is to be used internally

-	Reinforcement : RIW Toughseal Reinforcing Tape.

-	Blinding : Not required.

or to provide ‘key’ for finishes

- Blinding: RIW Aggregate, Grade 1.

or to provide a wearing surface

-	Blinding :  RIW Aggregate, Grade 2.

EXECUTION

J30/205A	SUITABILITY OF SUBSTRATE

-	Substrates generally :

-	Smooth, even textured, clean, dry and frost free.

-	Within tolerances for level and surface regularity.

-	Vertical and horizontal surfaces : Correctly prepared and free from irregularities.

-	Moisture content and stability of substrate : Must not impair integrity of finished tanking / damp proofing.

-	Preliminary work : Complete including :

-	Chases.

-	External angles.

-	Formation of upstands and kerbs.

-	Movement joints.

-	Penetrations / Outlets.

206	ADHESION TESTING

-	Tensile bond strength : Test in accordance with BS EN ISO 4624.

-	Test results : Submit.

J30/210 	COATING APPLICATION

-	Adjacent surfaces exposed to view in finished work : Protect.

-	Coatings :

-	Apply in dry atmospheric conditions when substrate is dry.

-	Uniform, continuous coverage. Do not allow to pool in hollows.

-	Firmly adhered to substrate and free from imperfections.

-	Prevent damage to finished coatings.

-	Penetrations: Impervious.

-	Final covering: Apply as soon as possible after coating has hardened.

J30/220	COLD APPLIED COATINGS

-	Thinning : Not permitted unless recommended by manufacturer.

-	Successive coats :

-	Allow to dry before applying next.

-	Apply at right angles to previous.

235	MODIFIED COATINGS

-	Air and surface temperatures : Do not apply if below minimum recommended by coating manufacturer.

-	Curing : Keep dry until fully cured.

J30/260 	JUNCTIONS WITH DPC’s

-	DPC’s : Clean, all edges fully exposed.

- Application : Fully coat dpc, and overlap adjacent surfaces by 75mm minimum.

J30/270	BLINDING

-	Coatings : Blind whilst tacky.

-	Surplus material : Remove when coatings are completely dry.